

TEST REPORT

**Tested by:** Jonathan Tow, P. Eng **Testing Location:** Powertech Labs Inc.

**Part:** PC2110 and PC3710 Perimeter Channel  
  
**Test Setup:**

Yield Location

F1

F2

**Conclusions / Observations:**

The Perimeter Channels, PC3710 and PC2110, yield at the same location under the same load.

With the glazing stop installed, the perimeter channel yields under a load of 6.2 kN/m with 5mm of deflection.

Without the glazing clip installed, the perimeter channel yields under a load of 21 kN/m with 4mm of deflection.

All of the deformation is isolated to the location indicated in the image above, the glazing clip does not deform plastically.